# Development of innovative biopolymer materials

### Introduction

The development of innovative biopolymer materials has been underway for a number of years, and continues to be an area of interest for many scientists. In 1996, shipments from the Canadian Plastic Industry increased by 10.6% from 1995 levels (Charron 1999), to $9.1 billion.Fomin (2001) reported that the end of the 20th century saw the worldwide production of synthetic plastics reach 130 million t/year, while the demand for biodegradable plastics is reported to be growing by 30% each year (Leaversuch 2002). European countries have reported an estimated average usage of 100kg of plastic per person each year (Mulder 1998).

Synthetic plastics are resistant to degradation, and consequently their disposal is fuelling an international drive for the development of biodegradable polymers. As the development of these materials continues, industry must find novel applications for them.

The biodegradable polymer that can be broken into small segments by enzymes. The enzymes are produced by microorganism.the carbon bond of chain grouth polymer and catalyzed reaction. Inert to the enzymes catalyzed reaction so, they are nonbiodegradable unless bond that can be broken by enzymes are broken by enzymes are inserted into the polymer when,the polymer is buried as waste,micro organisms present in the ground can be degrade the polymer one method of making the polymer biodegradable invalves inserting hydrolysable ester group into the polymer[1]

Reduction in theconsumption of sources, reuse of existing materials, and recycling of discarded materials must all be considered.Polymer materials are solid, non-metallic compounds of high molecular weights. (Callister 2000). They are comprised of repeating macromolecules, and have varying characteristics depending upon their composition. Each macromolecule that comprises a polymeric material is known as a mer unit. A single mer is called a monomer, while repeating mer units are known as polymers. A variety of materials (both renewable and non-renewable) are employed as feedstock sources for modern plastic materials. Plastics that are formed from non-renewable feedstocks are generally petroleum-based, and reinforced by glass or carbon fibers (Williams etal. 2000). Renewable resource feedstocks include microbially-grown polymers and those extracted from starch. It is possible to reinforce such materials with natural fibers, from plants such as flax, jute, hemp, and other cellulose sources.

### BIODEGRADABLE POLYMER

The hige chemical stability of many polymer is both a blessing and a curse.heat resistance,wear resistance,and long life are valuable characteristics of clothing fiber .bicycle helmets,underground pipes,food wrappers,and many other items.yet when those items outlive their usefulness,disposal can become a problem.

Recycling of unwanted polymer is the best solution,and six type of plastics in common use are frequently stamped with identifying codes assigned by the society of the plastics industry.after sorting by the type ,the item to be recycled are shredded into small chips, washed,dried,and melted for reuse.soft-drink bottles,for instance,are made from recycled poly(ethylene terephthalate),trash bages are made from recycled low-density polyethylene and mixed plastics.

### RECYCLABLE PLASTICS

### POLYMER RECYCLING CODE USE

Poly(ethylene terepthalate) 1-PET Soft-drink bottles

Hige density polyethylene 2-HDPE Bottles

Poly (vinyl chloride) 3-V Food mats

Low density polyethylene 4-DPE Grocery bags

Polypropylene 5-PP Furniture

Polystyrene 6-PS Molded articles

Mixed plastics Benches,plastic lumber

### BIODEGRADABILITY OF POLYMERS

The American Society for Testing of Materials (ASTM) and the International Standards Organization (ISO) define degradable plastics as those which undergo a significant change in chemical structure under specific environmental conditions. These changes result in a loss of physical and mechanical properties, as measured by standard methods. Biodegradable plastics undergo degradation from the action of naturally occurring microorganisms such as bacteria, fungi, and algae. Plastics may also be designated as photodegradable, oxidatively degradable, hydrolytically degradable, or those which may be composted. Between October 1990 and June 1992, confusion as to the true definition of “biodegradable” led to lawsuits regarding misleading and deceitful environmental advertising (Narayan et al. 1999). Thus, it became evident to the ASTM and ISO that common test methods and protocols for degradable plastics were needed. There are three primary classes of polymer materials which material scientists are currently focusing on. These polymer materials are usually referred to in the general class of plastics by consumers and industry. Their design is often that of a composite, where a polymer matrix (plastic material) forms a dominant phase around a filler material. The filler is present in order to increase mechanical properties, and decrease material costs.

### DEFININD BIODEGRADABILITY

Biodegradation depending on whether the conditions are

aerobic or anaerobic, respectively.

Aerobic biodegradation:

CPOLYMER + O2 → CO2 + H2O + CRESIDUE + CBIOMASS (1.1)

Anaerobic biodegradation:

CPOLYMER → CO2 + CH4 + H2O + CRESIDUE + CBIOMASS (1.2)

Complete biodegradation occurs when no residue remains, and complete mineralisation is established when the original substrate, (CPOLYMER in this example), is completely converted

into gaseous products and salts. However, mineralisation is a very slow process under

natural conditions because some of the polymer undergoing biodegradation will initially

be turned into biomass [11]. Therefore, complete biodegradation and not mineralisation

is the measurable goal when assessing removal from the environment.

### The Chemistry of Biodegradable Polymers

Any discussion of the chemistry of biodegradable polymers will inevitably invoke adiscussion of natural and synthetic polymers as well as a discussion of polymers derived from renewable and non-renewable resources. In order to put these matters to restimmediately it should be noted that biodegradable polymers may be naturally occurring or they may be synthesized by chemical means. In addition the feedstocks used to produce the polymers may come from the processing of crops grown for the purpose or the by products of other crops (so called renewable resources) or they may come from petro-chemical feedstocks (so called non-renewable resources). Whether renewable sources of feedstocks are better than non-renewable sources is a judgment that cannot be made without carrying out an environmental impact analysis on each source. For example ; the growing of agricultural crops may involve the application of fertilizers,herbicides and pesticides which may leave a deep environmental footprint. Unless appropriate soil management practices are in place the soils risk severe depletion of nutrients, microorganisms etc. In addition chemical or biochemical processes usually are required to extract and purify the polymer. These processes may require water, energy and chemical or biological additives. They also produce wastes which require treatment and disposal.

### Naturally Occurring Polymers

The history of man is strongly linked to a wide variety of naturally occurring polymers.For most of this history the fact that these substances were polymers was not known. In many quarters this ignorance persists. The natural polymers fall into four broad groups:

- Polysaccharides Starch, Cellulose

- Proteins Gelatin, Casein, Silk, Wool

- Polyesters Polyhydroxyalkanoates

- Others Lignin, Shellac, Natural Rubber

It cannot be automatically assumed that natural polymers, “are beautiful for

environmental degradation”. The rate of degradation and the formation of the ultimate metabolites depend very much on the structural complexity of the material and the environmental conditions selected for the degradation trial.

### Synthesized Biodegradable Polymers.

There are many polymers produced from feedstocks derived from petrochemical or biological resources that are biodegradable. Many of these have been around for some time either as curiosities or materials of commerce filling very special market niches as for example “dissolving” suture material used in the medical field. Others such as certain biopolyesters attempted for many years to compete against the standard commodity resins but failed to make significant market advances due to their high prices.The introduction of new materials, unless niche oriented, is generally caught in the volume, price conundrum. High sales volumes are not achievable because of high prices,but in order to reduce price costs must be reduced through the benefits that accrue from high volumes of production.In more recent times several sizable niche markets have opened for biodegradable plastics eg. bags for municipal composting. In addition the potential value of wastes from industries such as sugar refining as feedstocks has been recognized. The drive for sustainable development has promoted interest in the development of chemicals derived from the farming of particular crops among a number of large multi-national corporations. As a result the capital resources, marketing expertise and capability in research and development are coming together to lay the foundation of a new industry.As previously stated there are a number of biodegradable synthetic resins. The list includes:

- Polyalkylene esters

- Polylactic acid and its copolymers

- Polyamide esters

- Polyvinyl esters

- Polyvinyl alcohol

- Polyanhydrides

Each of these has its particular properties and potential applications. Polyvinyl alcohol is

widely used because of its solubility in water. Polylactic acid is growing in terms of production volume and applications. All of the materials in the list have been found to exhibit degradation promoted by microorganisms often coupled to chemical and/or mechanical degradation.

### BIODEGRADABLE POLYMER CLASSES

Three broad classes of commercially important biodegradable polymers are discussed :-

- unmodified polymers that are naturally susceptible to microbial-enzyme attack,

- synthetic polymers, primarily polyesters, and

- naturally biodegradable polymers that have been modifi ed with additives and fi llers.

Naturally biodegradable polymers produced in nature are renewable. Some synthetic

polymers are also renewable because they are made from renewable feedstocks, for example polylactic acid (PLA) is derived from agricultural feedstocks.

### 1.Naturally Biodegradable Polymers :-

Natural polymers are produced in nature by all living organisms. Biodegradation reactions are typically enzyme-catalysed and occur in aqueous media. Natural macromolecules containing hydrolysable linkages, such as protein, cellulose, and starch, are generally susceptible to biodegradation by the hydrolytic enzymes of microorganisms. Thus the hydrophilic/hydrophobic character of polymers greatly affects their biodegradability. It also has a great impact on their performance and durability in humid conditions. The major category of biodegradable polymers consists of those with hydrolysable linkages along the polymer chain backbone: polyesters, polyamides, polyureas, polyanhydrides, poly(amide-enamine)s, polyurethanes (PU), and polyphosphazene. Outside of natural fi bres like wool and silk, polysaccharides such as starch are the most prevalent naturally biodegradable polymers in commercial use. Starch, or plant nutrient material, is composed of two polysaccharides: α-amylose and amylopectin. The primary structure of α-amylose is linear because of the exclusive α (1-4) linkages between the D-glucose monomers α-Amylose typically has a MW of 1.6 x 105 to 2.6 x 106 [8]. Amylopectin is branched because of the presence of α (1-6) linkages as well as the α (1-4) linkages,

### 2.Synthetic Biodegradable Polymers :-

While natural polymers are produced by living organisms, synthetic biodegradable polymers are only produced by mankind. Biodegradation reactions are the same for both, i.e., typically enzyme-catalysed and occurring in aqueous media. The major category of synthetic biodegradable polymers consists of polyesters with hydrolysable linkages along the polymer chain backbone. PVOH is also reported to be biodegradable. Interest in simple aliphatic polyesters such as PLA was pioneered by Carothers in the 1930s . The susceptibility of these polymers to hydrolytic degradation led to DuPont discontinuing work in this area. The ability of the human body to degrade these materials led to medical applications in the 1970s; the simplest poly(α-hydroxyacid), polyglycolic acid (PGA), has been successfully used in degradable surgical sutures . PGA is usually obtained by polymerising diglycolide with a tin catalyst. Similarly, PLA can be obtained from dilactide by stannous octoate catalysed, ring-opening polymerisation. Biodegradable polyesters such as PLA, PGA, and their copolymers have been used widely in medicine and surgery for the controlled release of drugs, biodegradable surgical sutures, and implants for fi xation of fractures, primarily because of their high biocompatibility . In orthopaedic surgery, biodegradable fi xation devices such as screws, plates, and pegs have the advantage of temporarily securing bone prostheses. The device is eventually absorbed by the body after bone tissue growth into the porous matrix structure of the prosthesis effectively affi xes the implant to the bone.

### 3.Modified Naturally Biodegradable Polymers :-

### C arbohydrates are naturally occurring organic compounds that are related to simple sugars. They are extremely widespread in plants, accounting for as much as 80% of plant dry weight. Polysaccharides are biodegradable polymers made up of simple carbohydrate subunits, i.e., saccharides such as glucose. The linear polysaccharide, cellulose, is probably the single most abundant organic compound on earth and it is the chief structural component of plant cells. Enzymes (cellulases) that can catalyse the degradation of cellulose to glucose are common in microorganisms. Starch is the second most abundant polysaccharide. In animals it is the chief source of carbohydrates; in plants it is present in the form of small insoluble starch granules. Polysaccharides such as starch readily gelatinise in hot water to form a paste that can be cast into fi lm. Such fi lms, however, are sensitive to water and become brittle on drying. Less brittle fi lms can be produced by combining polysaccharide with other materials such as plasticisers and synthetic polymers. Since the 1970s, numerous attempts have been made to enhance the biodegradability of synthetic polymers by incorporating polysaccharide-derived materials . The microstructure plays a fundamental role in determining the biodegradation rate of this class of products.

### METHODS OF BIODEGRADATION

Just as important as the way in which a material is formed is the way in which it is degraded. A general statement regarding the breakdown of polymer materials is that it may occur by microbial action, photodegradation, or chemical degradation. All three methods are classified under biodegradation, as the end products are stable and found in nature. Many biopolymers are designed to be discarded in landfills, composts, or soil. The materials will be broken down, provided that the required microorganisms are present. Normal soil bacteria and water are generally all that is required, adding to the appeal of microbially reduced plastics (Selin 2002). Polymers which are based on naturally grown materials (such as starch or flax fiber) are susceptible to degradation by microorganisms. The material may or may not decompose more rapidly under aerobic conditions, depending on the formulation used, and the microorganisms required. Photodegradable polymers undergo degradation from the action of sunlight (ASTM 883-96). Inmany cases, polymers are attacked photochemically, and broken down to small pieces. Further microbial degradation must then occur for true biodegradation to be achieved. Polyolefins (a type of petroleum-based conventional plastic) are the polymers found to be most susceptible to photodegradation. Proposed approaches for further developing photodegradable biopolymers includes incorporating additives that accelerate photochemical reactions (e.g. benzophenone),modifying the composition of the polymers to include more UV absorbing groups (e.g. carbonyl), and synthesizing new polymers with light sensitive groups (Andreopoulos et al. 1994). Anapplication for biopolymers which experience both microbial and photodegradation is in the use of disposable mulches and crop frost covers. Some biodegradable polymer materials experience a rapid dissolution when exposed to particular (chemically based) aqueous solutions. As mentioned earlier, Environmental Polymer's product Depart is soluble in hot water. Once the polymer dissolves, the remaining solution consists of polyvinyl alcohol and glycerol. Similar to many photodegradable plastics, full biodegradation of the aqueous solution occurs later, through microbial digestion. The appropriate microorganisms are conveniently found in wastewater treatment plants (Blanco 2002). Procter & Gamble has developed a product similar to Depart, named Nodax PBHB.

### The proposed sequence for biodegradation is: -

1. The polysaccharide material is fi rst consumed by microorganisms, a process that also increases the surface area of the synthetic polymer and weakens the polymer matrix. 2. The remaining synthetic polymers break into smaller fragments as a result of other environmental mechanisms, which are eventually small enough for assimilation by microorganisms. Reportedly even PE is biodegradable if the MW is below 500 [2]. The dominant commercial starch-based biodegradable polymers are marketed by Novamont in Italy under the name Mater-Bi®. This starch-based technology is unique because the modifi cation goes beyond conventional compounding. In the Mater-Bi® technology, starch is destructurised by applying suffi cient work and heat to almost completely destroy the crystallinity of amylose and amylopectine in the presence of macromolecules able to form a complex with amylose. Novamont produces several different classes of Mater- Bi®, all containing starch with different classes of synthetic components such as PCL [12]. The material obtained is available for making fi lm and sheets, foams, and injection moulding.

### Modifi ed starch-based polymers are promoted as potential solutions to the current litter/

### municipal solid-waste management problems in as much as they serve two purposes:

1. Using polysaccharides that are naturally derived macromolecules from renewable sources reduces the amount of plastic needed from non-renewable petrochemical sources. 2. Incorporation of the polysaccharide enhances the overall biodegradability of the combined product. Another argument for using agriculturally based additives is the potential reduction in farm subsidies it could allow. For example, use of corn starch may provide another use for the nation's corn production.

### Mechanisms of Polymer Degradation

Biodegradation is usually defined as degradation caused by biological activity (especially enzymic action), it will usually occur simultaneously with - and is sometimes even initiated by - abiotic degradation such as photodegradation and simple hydrolysis.

### Degrada tion of polymer is of two type

### 1.Non-biological Degradation of Polymers

A great number of polymers are subject to hydrolysis, such as polyesters, polyanhydrides, polyamides, polycarbonates, polyurethanes, polyureas, polyacetals, and polyorthoesters. Different mechanisms of hydrolysis have been extensively reviewed; not only for backbone hydrolysis, but also for hydrolysis of pendant groups [12, 13]. The necessary elements for a wide range of catalysis, such as acids and bases, cations, nucleophiles and micellar and phase transfer agents, are usually present in most environments. In contrast to enzymic degradation where a material is degraded gradually from the surface inwards (primarily because macromolecular enzymes cannot diffuse into the interior of the material), chemical hydrolysis of a solid material can take place throughout its cross section except for very hydrophobic polymers.

### Important features affecting chemical polymer degradation and erosion include:

(a) the type of chemical bond, (b) the pH, (c) the temperature,

### Biodegradability of Polymers - Mechanisms and Evaluation Methods

(d) the copolymer composition, and (e) water uptake (hydrophilicity). These features will not be discussed here, but have been cov

### 2. Biological Degradation of Polymers

Polymers represent major constituents of the living cells which are most important for the metabolism (enzyme proteins, storage compounds), the genetic information (nucleic acids), and the structure (cell wall constituents, proteins) of cells. These polymers have to be degraded inside cells in order to be available for environmental changes and to other organisms upon cell lysis. It is therefore not surprising that organisms, during many millions of years of adaptation, have developed various mechanisms to degrade naturally occurring polymers. For the many different new synthetic polymers that have found their way into the environment only in the last fi fty years, however, these mechanisms may not as yet have been developed. There are many different degradation mechanisms that combine synergistically in nature to degrade polymers. Microbiological degradation can take place through the action of enzymes or by products (such as acids and peroxides) secreted by microorganisms (bacteria, yeasts, fungi, etc). Also macro-organisms can eat and, sometimes, digest polymers and cause mechanical, chemical or enzymic ageing. Two key steps occur in the microbial polymer degradation process: fi rst, a depolymerisation or chain cleavage step, and second, mineralisation. The fi rst step normally occurs outside the organism due to the size of the polymer chain and the insoluble nature of many of the polymers. Extracellular enzymes are responsible for this step, acting either endo (random cleavage on the internal linkages of the polymer chains) or exo (sequential cleavage on the terminal monomer units in the main chain). Once suffi ciently small size oligomeric or monomeric fragments are formed, they are transported into the cell where they are mineralised. At this stage the cell usually derives metabolic energy from the mineralisation process. The products of this process, apart from adenosine triphosphate (ATP), are gasses, (e.g., CO2, CH4, N2, H2), water, salts and minerals, and biomass. Many variations of this general view of the biodegradation process can occur, depending on the polymer, the organisms, and the environment. Nevertheless, there will always be, at one stage or another, the involvement of enzymes.

### Measuring Biodegradation of Polymers :-

Biodegradationdoes not only depend on the chemistry of the polymer, but also on the presence of thebiological systems involved in the process. When investigating the biodegradability of a material, the effect of the environment cannot be neglected. Microbial activity, and hence biodegradation, is infl uenced by:

- the presence of microorganisms

- the availability of oxygen

- the amount of available water

- the temperature

- the chemical environment (pH, electrolytes, etc.)

In order to simplify the overall picture, the environments in which biodegradation occurs are basically divided in two environments: (a) aerobic (with oxygen available) and (b) anaerobic (no oxygen present). These two, can in turn be subdivided into (1) aquatic and (2) high solids environments. presents schematically the different environments, with examples in which biodegradation may occur

### APPLICATIONS FOR BIODEGRADABLE POLYMERS :-

Research and development is only a portion of the work that is done in order to introduce the use of biodegradable polymer materials. The design of such materials usually begins with a conceptual application. It may be expected to replace an existing material, or to complement one. Sectors where applications for biopolymers have introduced include (but are not limited to)medicine, packaging, agriculture, and the automotive industry. Many materials that have beendeveloped and commercialized are applied in more than one of these categories.

Biopolymers that may be employed in packaging continue to receive more attention than thosedesignated for any other application. All levels of government, particularly in China (Chau et al 1996) and Germany (Bastioli 1998), are endorsing the widespread application of biodegradable packaging materials in order to reduce the volume of inert materials currently being disposed ofin landfills, occupying scarce available space. It is estimated that 41% of plastics are used inpackaging, and that almost half of that volume is used to package food products.

BASF, a world leader in the chemical and plastic industry, is working on further development ofbiodegradable plastics based upon polyester and starch (Fomin et al. 2001). Ecoflex is a fullybiodegradable plastic material that was introduced to consumers by BASF in 2001. The

material is resistant to water and grease, making it appropriate for use as a hygienic disposablewrapping, fit to decompose in normal composting systems. Consequently, Ecoflex has found anumber of applications as a packaging wrap.

Environmental Polymers (Woolston, Warrington, UK) has also developed a biodegradable

plastic material. Known as Depart, the polyvinyl alcohol product is designed for extrusion,

injection molding, and blow molding. Depart features user-controlled solubility in water, which isdetermined by the formulation employed. Dissolution occurs at a preset temperature, allowing the use of Depart in a variety of applications. Examples include hospital laundry bags which are “washed away” allowing sanitary laundering of soiled laundry, as well as applications as disposable food service items, agricultural products, and catheter bags (Blanco 2002).

The renewable and biodegradable characteristics of biopolymers are what render them

appealing for innovative uses in packaging. The end use of such products varies widely. For example, biodegradable plastic films may be employed as garbage bags, disposable cutlery and plates, food packaging, and shipping materials. Guan and Hanna (2002) documented how biodegradable loose-fill packaging materials may be developed from renewable biopolymers such as starch. The starch material is treated by an acetylation process, chemical treatments, and post-extrusion steaming. Mechanical properties of the material are adequate, and true biodegradability is achieved.

The biopolymer materials suited for packaging are often used in agricultural products. Ecoflex, in particular, sees use in both areas. Young plants which are particularly susceptible to frostmay be covered with a thin Ecoflex film. At the end of the growing season, the film can be worked back into the soil, where it will be broken down by the appropriate microorganisms. Li etal. (1999) concluded that the use of a clear plastic mulch cover immediately following seeding increases the yield of spring wheat if used for less than 40 days. Therefore, plastic films that begin to degrade in average soil conditions after approximately one month are ideal candidates as crop mulches. Agricultural applications for biopolymers are not limited to film covers. Containers such as biodegradable plant pots and disposable composting containers and bags are areas of interest (Huang 1990). The pots are seeded directly into the soil, and breakdown as the plant begins to grow. Fertilizer and chemical storage bags which are biodegradable are also applications that material scientists have examined. From an agricultural standpoint, biopolymers which are compostable are important, as they may supplement the current nutrient cycle in the soils wherethe remnants are added.The medical world is constantly changing, and consequently the materials employed by it alsosee recurrent adjustments. The biopolymers used in medical applications must be compatible with the tissue they are found in, and may or may not be expected to break down after a giventime period.

### Result and Conclusions

There are many polymers produced from feedstocks derived from petrochemical or biological resources that may be demonstrated to be biodegradeable using standardized test methods.

ASTM Standard D 6400-99 sets a “Standard Specification for Compostable Plastics” which is used by the US Composting Council and the Biodegradable Products Institute as the principal criterion which must be achieved in order to use their logo defining a compostable plastic product.

Biodegradeable plastic products are, at present, more expensive than products manufactured from commodity resins and hence their application and acceptance is based on demonstrated “value in use”. In addition the user is advised to carry out where-ever possible a life cycle assessment of the product and its application in order to assure that the product provides true environmental benefit and not simply convenience. Sources of products may be readily determined by an inter-net search using “biodegradable plastics” or “compostable plastics” as key words.