# Molecular electronics and photovoltaics

### Acknowledgements

I would like to thank Dr. Ben Robinson for his help and support throughout the duration of the literature review. I would also like to thank Prof. Geoff Ashwell for his guidance as well as Aled and Susan for their support.

### Area of Study

Electronic components made of conventional semiconductor materials face fundamental size, power and speed limits. A new approach is required for fabrication of future devices structures; molecular electronics is a possible solution. Molecules can act as wires, diodes and ultimately transistors as well as components in sensors and photovoltaics.

Systematically changing the components within the device should result in change of the rectification ratio. This is a result of controlling the band gap structure by coupling accepting and donating moieties and in some cases steric hindrance effects.

The literature addressed will be predominantly scientific journals and textbooks', ensuring that current knowledge is addressed.

### Introduction

Electronic components made of conventional semiconductor materials face fundamental size limits. A new approach is required for future devices; molecular electronics is one of the possible solutions. Molecular electronics popularity has been amplified greatly as the demand for smaller, more powerful devices increases[1]. In 1965, G.E. Moore predicted the miniaturisation of integrated electronics; that the number of components per integrated function would increase exponentially over time (Figure 1). To accommodate this miniaturisation, fabrication techniques such as Self Assembled Monolayer and Langmuir Blodgett need to be improved. This project focuses on the synthesis and characterisation of two molecular wires composing of systematically changed components and investigating their current output and variations.

There are two predominant approaches to molecular electronics; Conventional semiconductor materials currently use the top-down approach. This is where progressively smaller pieces of matter are manipulated by photolithography and related techniques[2]. These silicon chips are present in most electronic devices including PC's, phones and satellites. Major problems arising from the miniaturisation of top-down approach electronics include charge leakage from the insulating SiO2 layer. It soon will no longer be feasible to continue miniaturising the silicon based electronic devices. Due to this the need to advance the more adaptable bottom-up approach is imminent.

The method used within this project is the bottom-up approach comprising of a novel step by step assembly of two molecular wires containing three components (Figure 2).

This increase in rectification is due to the p-orbital's initially being overlapped creating a delocalised area where electrons can travel. Once a group such as benzene has been introduced the p-orbital's no longer align in a way that they can interact, this effectively breaks the conjugation in the wire and therefore the pathway for the electrons to travel, causing rectification.

This project proposes the synthesis and characterisation of previously unreported wires using the novel 'bottom-up' method for constructing the complex, asymmetric SAMs as first proposed by Ashwell et al.[3] The interactions between acceptor and donor groups within the wire will be illustrated and future systems with improved rectification predicted. Within this literature review, each fabrication approach will be looked at in the context of current knowledge and compared to establish the paramount technique for nanofabrication for future use in molecular electronics.

### Literature Review

### Top-Down Approach:

The top-down approach applies to creating organic and inorganic architectures, by the use of ion and electron, photon and atom beams to sculpt matter from macroscopic to nanoscopic dimensions.[4] Currently, over 100 million transistors can be accommodated on just a few square centimetres of silicon, resulting in greater computing power and performance in devices such as PC's. In most electronic devices these silicon chips are now present.[5] Advanced nanopatterning, such as electron beam lithography and focused-ion beam lithography can write features sizes below 10nm.[6] An advantage of top-down fabrication is that device attributes such as electrical contacts are well developed and can be controlled; another advantage is the commercial availability of high-quality silicon-on-insulator substrates for silicon nanowires.[7] Several developments have been made in the past year, yet the approach still shows great limitations for the future.

Chen et al (2009) propose a new low-cost top-down silicon nanowire fabrication technology requiring only conventional micro fabrication processes including microlithography, oxidation and etching. These wires can be made in facilities without the need for expensive equipment. With lateral dimensions ranging from 200nm to 10-20nm and lengths up to ~100µm can be produced with near perfect monocrystalline cross sections.6

This novel silicon nanowire fabrication proposed by Chen et al. (2009) using only two microlithography steps utilizing plane dependent wet etching (PDE) and a conventional micro fabrication process involving gate oxidation and contact metallization. Figure 4 shows the simple fabrication process as a diagram.

The popular top-down fabrication of silicon nanowires is to initially reduce the silicon device layer thickness, followed by the required nanopatterning. This however results in thin electrical contact regions can lead to high contact resistances.7 A great advantage of Chen et al. (2009) new reduction method is that the electrical contact regions are not reduced in thickness providing low resistance contacts, shown in wires with wafer-scale yields greater than 90%. This method is effective and not expensive; nonetheless it still has size and time limitations.

Another novel, low-cost top-down nanowire fabrication has been proposed by Tong et al. (2009). These wires can be fabricated without the use of nanolithography in conventional micro technology clean room facilities. Lateral widths of ~100nm, thicknesses of ~20nm and lengths up to 2mm can be produced.7

A novel silicon nanowire fabrication is proposed by Tong et al. (2009) utilizing angled thin-film deposition and etching with a single photolithography step. This novel fabrication technique is known as deposition and etching under angles (DEA); improved dimensional control can be seen when the stencil structure is patterned directly upon the wafer surface, with the use of precisely defined cavity which permits a controlled removal of the waste material with an angled wafer-level ion beam this minimises lateral spread of the deposited metal.7 The metallic nanowire is then used as a hard mask to transfer the pattern to the top layer of a silicon-on-insulator wafer by dry etching to produce wafer-scale silicon nanowires, with lateral dimensions below 100nm.7

Although these developments are promising with regards to achieving miniaturisation, they are still a distance from achieving the same size as the bottom-up technique. It is becoming clear that the top-down has large limitations, including large cost increases for advanced fabrication techniques when the components reach the nanoscale size.2 At such a scale, problems include charge leakage from the insulating silicon dioxide layer,[8] as well as the need for new fabrication techniques to accommodate such small-scale systems. Eventually, it will no longer be effective to continue reducing these silicon-based electronic devices, thus generating a need for the development of alternative fabrication methods such as the bottom-up approach.

### Bottom-Up Approach:

The bottom-up approach applies to building organic and inorganic architectures atom-by-atom or molecule-by-molecule. This approach is the use of nanoscale electronics; relating to systems between 1-100 nm. The simplest of this is one or more molecules sandwiched between two electrodes which provides a method for electron transport can be used as wires, diodes3 and ultimately transistors. Bottom-up manufacturing provides components made of single molecules held together by covalent forces that are much stronger than the forces that hold together macro-scale components.[9] The two techniques used to produce nanostructures using the bottom-up approach are Self-Assembled Monolayer and Langmuir Blodgett.

Bottom-up nanofabrication provides high quality materials and is simple to complete. However electrical contact formation is problematic, making it difficult to construct functional devices.6

### Self-Assembled Monolayer:

The term self-assembly entails spontaneity, a structure builds itself from molecular construction units and an ordered pattern forms from a disordered state due to Van der Waals forces.[10] The synthesis of the two wires within the project is completed by self assembled monolayers (S.A.Ms); where the component structures are chemisorbed via gold-thiol linkages. Including gold, thiol groups chemisorbs to form strong covalent bonds with other metals such as platinum[11] and palladium[12].

The advantages of using S.A.Ms are the control of the size and electrical properties of the molecular wire. This allows control over the choice of the layers which can be seen in figure 2 with the change of layer 3 between the two wires.

The components of the wires will be systematically changed to see if the rectification ratio is affected by donor/acceptor strength and steric hindrance. To be successful in practical electronic devices the organic structure must allow current to pass in one direction more than the other this means there must be rectification within the wire. The adjacent donor and acceptor moieties are separated by linking groups; such as layer two (Figure 2) that inhibits the movement of electrons between the acceptor and donor moieties. This structure characteristic means the electrons will move easily towards the electron deficient area rather than the electron rich causing rectification.

Aviram and Ratner in 1974 proposed the first organic rectifying system, consisting of a simple electron accepting group and donating group separated by an insulating ?-bridge[13] which ensures the donor and accepting moieties do not interact electronically.

Rectification depends upon the molecule being sterically hindered, which breaks the conjugation by imposing a non-planar D-?-A structure. The donor and acceptor on opposite sides of the ?-bridge are preserved. Due to this at forward bias; the electrons tunnel from the cathode to the lowest unoccupied molecular orbital of the acceptor on one side, and from the highest occupied molecular orbital of the donor to anode on the other side.[14]

Research carried out by Ashwell et al. has shown the effect of steric hindrance upon rectification.[15] An example can be seen in Figure 5, showing that with an increase in dihedral angle of the central HC=CH bridge of 31° to 61°, the rectification value increases from approximately 18 to approximately 130 at ± 1V. A system with little twist (10°) exhibits no rectification: 1 at ± 1V.

The surface of the electrode the wire is self assembled on plays an important part in the results achieved. Weiss et al. reported that electrical current through SAMs prepared on as-deposited Ag surfaces were often orders of magnitude higher than that found on atomically flat Ag surfaces. Devices that were prepared from as-deposited (rough) surfaces exhibited higher rates of failure.[17]

The main advantages of self-assembled monolayers is the strong covalent bond between the reactive headgroup and the substrate, this makes the wires more stable than that of wires fabricated via Langmuir-Blodgett and the ability to choose the layers within the wire. The disadvantages of self-assembled monolayers are the method is time consuming, expensive and not yet producible on a large scale.

### Langmuir-Blodgett Technique:

The Langmuir-Blodgett technique method requires spreading the molecular film at the air/water surface interface and then compressing the molecular film to the desired area prior to transferring the film to the solid substrate to produce the monolayer. The low output of this method prevents it becoming a manufacturing technique, and it is limited to amphiphilic molecules. The facility to control the area per molecule is a large advantage. This technique provides complex and functional molecules. The monolayers fabricated are defect free; providing effective bilayers and multilayer films when prepared.

Ashwell et al. (1990) proposed the first system in which a ?-bridged metal?LB monolayer?metal junction was investigated.[18] The required ?-bridges are easier to synthesise than ?-bridges. ?-bridges create a more stable system; this rigidness results in more ordered packing. If the donor and acceptor orbitals are twisted out of plane this breaks conjugation, because of this a barrier is formed which confines electrons to either side of the ?-bridge. This can be seen in Figure 7 where rotations occur about the single bonds which link the acceptor and donor to the ?-bridge. It is essential that donor-electron bridge-acceptor structure is present for rectification to occur.

An advantage of Langmuir-Blodgett films over the Self-Assembled Monolayers is the compatibility of the Langmuir-Blodgett technique with a large range of metal-organic interfaces. This is achieved through the large number of polar functional groups which can be physically or chemically adsorbed onto a wide array of substrates.[19]

### Applications in Photovoltaics:

The interest in solar power has increased greatly over time. Solar technologies are currently dominated by single-junction solar cells based on crystalline silicon that are assembled on large area molecules.[20] A new generation of photovoltaics is emerging, in particular the dye-sensitized solar cell (DSC). This new technique uses nanotechnology and molecular devices.

Dye-sensitized solar cells are based on the separation of charge carriers which is kinetically controlled by the chemical reactions involved for the dye sensitizer when light is adsorbed.[21] The task of light adsorption and charge carrier transport are separated in a dye-sensitized solar cell. The sensitizer which is the dye is chemically attached to the surface of a nanostructured wide band-gap semiconductor.21

Other semiconductor materials than silicon have been investigated for use in thin-film photovoltaic technologies, these are based upon inorganic and organic semiconductor materials that are more absorbing than crystalline silicon and can be processed directly onto large area substrates.20

Titanium dioxide has become the semiconductor of choice; it is cheap, abundant, nontoxic and biocompatible.[22] Using TiO2 as a semiconductor material has been reported since 1991 where a novel dye-sensitized solar cell with a conversion yield of 7.1% was accounted.[23] To be successful as a solar cell there needs to be high transparency and a large dye adsorption for the self-assembled solar cell which would increase the efficiency of the solar cell.

The ideal sensitizer for a single-junction photovoltaic cell should absorb all light below a wavelength of about 900nm. It should be grafted to the semiconductor oxide surface and inject electrons to the conduction band. The sensitizer should have a high redox potential so that it can be regenerated rapidly for example via an electron donation from the electrolyte. It should be stable enabling at least enough redox turnovers to last for 20 years in natural light.22 The most common sensitizer used is ruthenium complexes, these however are expensive so further sensitizers need to be developed.

The advantages of using nanotechnology for photovoltaics are the production of a low cost, efficient solar cell. This process provides little residue making it an ideal substitute for conventional silicon solar cells.

The molecular wires fabricated by SAMs will be manipulated by changing the first component of the wire, and deposited on TiO2 crystals to establish the molecular needs for developing new DSCs.

### Conclusions

Each technique described has individual advantages and disadvantages. These disadvantages need to be weighed up to establish the most promising technique for the future. For the present the most beneficial area of research is that of the bottom-up approach; as the size limitations for the top-down approach are too great. This corresponds with predictions from physicist Richard Feynman who was one of the first to predict the future of molecular electronics, giving a lecture in December 1959 entitled 'There is Plenty of Room at the Bottom'.

Top-down approach has several great limitations, including cost, charge leakage from the insulating silicon dioxide layer as well as the need for new fabrication techniques. It will no longer be effective to continue reducing these silicon-based electronic devices. However nanowires produced via a top-down approach are able to be produced on a large scale, providing repeatable results, this advantage needs to be developed in the bottom-up approach to provide a successful nanofabrication technique.

The main advantages of self-assembled monolayers are the strong covalent bond between the reactive headgroup and the substrate which in the case of this project a strong thiol bond between the headgroup sulphur and the gold substrate. This strong covalent bond makes the wires more stable than that of wires fabricated via Langmuir-Blodgett films and the ability to choose the layers within the wire. The disadvantage of self-assembled monolayers is the method is time consuming, expensive and not yet producible on a large scale. However these disadvantages can be lessened over time as electronic devices become smaller and more powerful, making research into self-assembled monolayers essential.

An advantage of Langmuir-Blodgett technique is the compatibility of the Langmuir-Blodgett fabrication technique with a large range of metal-organic interfaces, yet due to the low output it is not effective for use as a large scale nanofabrication technique.

The SAMs proposed in this project will provide a strong building block for further research developments for further more powerful molecular wires, and uses in photovoltaics by developing new cheaper sensitizers.

A possible interest for future research is combing the top-down and bottom-up approach, making further structures and thin nanochannels[24] as suggested by D. Mijatovic et al., (2005).

### References

- Moore, G.E., Electronics, 1965, 38, No 8

- Balzani, V., et al., Nanotoday, 2007, 2, 2, 18-25

- Ashwell, G.J., et al., Chem. Commun., 2007, 1254-1256

- Ozin. G. A., et al., Materials Today, 2009, 12, No. 5, 12-23

- Grill, L., et al., Nano. Lett., 2005, 5, No. 5, 859-863

- Chen, S., et al., ACSNano, 2009, 3, No 11, 3485-3492

- Tong, H. D., et al., Nano Lett., 2009, 9, No. 3, 1015-1022

- Tour, J.M., Acc. Chem. Res., 2000, 33, No. 11, 791-804

- Petty, M. C., Molecular Electronics From Principle to Practice, 2007, Wiley Publishing

- Ozin. G. A., et al., Materials Today, 2009, 12, No. 5, 12-23

- Shimazu, K., et al., Bull. Chem. Soc. Jpn., 1994, 67, No. 3, 863-865

- Love, J.C., et al., J. Am. Chem. Soc., 2003, 125, 2597-2609

- Aviram, A. and Ratner, M.A., Chem. Phys. Lett., 1974, 29, No. 2, 277-283

- Ashwell, G.J., et al., Phys. Chem. Chem. Phys., 2006, 8, 3314-3319

- Ashwell, G.J. and Mohib, A., J. Am. Chem. Soc., 2005, 127, 16238-16244

- Ashwell, G.J., et al., Phys. Chem. Chem. Phys., 2006, 8, 3314-3319

- Weiss E.A., et al., J. Am. Chem. Soc. 2007, 129, 4336–39

- Ashwell, G.J., et al, J. Chem. Soc., Chem. Commun., 1990, 1374-1376

- Villares, A., et al., Surface Science, 2008, 602, 3683-3687

- Kippelen, B. and Brédas, J.L., Energy Environ. Sci., 2009, 2, 251-261

- Polo, A.S., et al., Coordination Chemistry Reviews, 2004, 248, 1343-1361

- Gratzel, M. and Hagfeldt, A., Acc. Chem. Res. 2000, 33,269-277

- Gratzel, M. and O'Regan, B., Nature, 1991, 335, 737-739

- Mijatovic, D. et al., Lab Chip, 2005, 5, 492-500