# other notable effect of coking

2.5 OTHER NOTABLE EFFECT OF COKING

2.5.1 FEED COMPOSITION

The nature and composition of feed determines, it boiling point and structure. It is suggestive to the nature of coke formed on the reforming catalyst. It was noted that the usual feed to naphtha reforming unit contains [8, 9]:

Paraffins - 45-70 %

Naphthenes - 20-50 %

Aromatic - 5-15%

Olefins < 2%

It was also recognised that during reforming process, the amount of aromatic increase from the initial amount to a high degree and that of the paraffin's on the other hand decrease drastically with olefins almost disappearing from the content [9]. Thus it was observed that due to this different property, the hydrocarbon produces different effect on coke deposit. Light paraffins produce a little amount of cyclopentane which was observed to be a great coke precursor [10], while heavy paraffins which produce bicyclic compound with an interlock structure also served as a coke producer [10]

Catalyst deactivation increases with the length of paraffin chain attached to an aromatic ring. It was observed that a five ring atom is a precursor, thus if the feedstock contains a high concentration of aromatics compounds with 5C atom rings, more coke is produced and hence the catalyst deactivation is fast. The reason for this is due to the high reactivity of the 5 carbon atom ring with tendency to form heavy aromatics [11]

Trim and Beltramini et al [12, 13] reported the addition of paraffin to naphtha helps in minimising coke formation. Hence it was suggested that coke deactivation is a function of the number of carbon atom, when this is higher than 8.

Querini Fungi[14] demonstrated that when n-pentane is used as a feedstock in naphtha reforming the amount of coke formation was higher in the pre-sulphided Pt-Re catalyst because of increasing dehydrogenating reaction. Pieck et al disagrees but concludes that presulfurization produces an increase in coke on a Pt/Al203 catalyst whereas the reverse was observed on the Pt-Re catalyst [15]. However other researched shows that coke decreased after sulphurization [15].

The importance of feedstock in the reforming unit cannot be over emphasized, in an effort to understand coke precursor and devising an effective management technique in negating this phenomenon.