# Aim of experiment

The aim of this experiment is to identify and investigate the failure of plastic components by microscopy and other technique such as tensile test and FTIR.

### Materials and Equipments

- 5 Polypropylene samples

- Tensile test machine

- FTIR

- Reflected Light Microscope

### Theory

### Procedure

- The samples are identified and marked

- The samples are sent for tensile test

- The sample is then cut and prepared for FTIR and Reflected Light Microscope test with accordance to their preparation techniques

- The samples are tested with the FTIR and Reflected Light Microscope

### Discussion

### Tensile test

In our tensile test, we noticed that there is a difference in the sample 1and 2 versus sample 3, 4 &5. Sample 1&2 shown signs of a ductile failure whereas sample 3, 4 & 5 exhibited brittle failure. In Polypropylene, it is known that it will exhibit a brittle failure and not a ductile failure. With this, we are able to preliminary classify it as 2 distinct class of failure samples. One that exhibits normal failure and one group that exhibit unusual failure.

### FTIR

For all 5 samples, our FTIR matches all of them as isotatic Polypropylene. This means that the possibilities of contamination of materials are ruled out.

### Glass Transition Temperature

In sample 1 and 2, we found out that the Tg are generally lower by sample 3, 4 and 5 by around 10 degree Celsius. This are tell tales signs that the materials are degraded prior or during processing.

### Conclusion

In this experiment, we have successfully identified the problem to a certain extent, which could be due to degradation of the material prior or during processing. This problem need to be double confirmed using the fluorescence light microscope, which is not available to us at the time of testing.

By preliminary identifying this problem, we are able to provide a few possible solution to try to remedy this problem:

- Proper storage of raw materials before storage with accordance to manufacturer's specification

- Proper processing parameters with accordance to manufacturer's specification

- Incorporate an additional quality check for these defects in the manufacturing process

If by applying these initial remedies and no results are shown, we will suggest checking the raw materials that is supplied to manufacture if it had shown any similar problems.

In this experiment, we also learnt how to make use to multiple methods in pinpoint of the problems that a product could possibly have.

### References

- Lab Manual

- Lecture Notes for CP0006